## Slide 1: Comprehensive Study of Plasmonic Effects in Organic Solar Cells
1. Department of Electrical and Electronic Engineering,
The University of Hong Kong, Hong Kong
2. Department of Electrical and Computer Engineering,
University of Illinois, Urbana-Champaign,
Illinois 61801, USA
Emails: chchoy@eee.hku.hk (W.C.H. Choy); w-chew@uiuc.edu (W.C. Chew)
Wei E.I. Sha1 (沙威), Wallace C.H. Choy1 (蔡值豪), and Weng Cho Chew2 (周永祖)

## Slide 2: Organic Solar Cell (1)
organic solar cell
monocrystalline silicon solar cell
amorphous/polycrystalline silicon solar cell
Advances of solar cell technology

## Slide 3: Organic Solar Cell (2)
Thin-film organic solar cell
low-cost processing
mechanically flexible
large-area application
environmentally friendly
low exciton diffusion length
low carrier mobility

## Slide 4: Organic Solar Cell (3)
optical absorption
exciton diffusion
charge separation
charge collection
Working principle
increase interface area

## Slide 5: Plasmonic Organic Solar Cell
Why optical enhancement?
The thickness of the active layer must be smaller than the exciton diffusion length to avoid bulk recombination. As a result, the thin-film organic solar cell has poor photon absorption or harvesting. Plasmonic solar cell is one of emerging solar cell technologies to enhance the optical absorption.
nanoparticles: local plasmon
nanograting: surface plasmon

## Slide 6
X.H. Li, W.E.I. Sha, W.C.H. Choy, etc, J. Phys. Chem. C, 116(12), 7200-7206, 2012.
Plasmonic band edge boosted optical enhancement (theory and experiment)
finite-difference frequency-domain method (TE&TM)

## Slide 7
VIE-FFT method (BiCG-STAB)
concentration
dependent
2 fold increase in total absorption!
Near-field
Far-field
direction dependent
k
k
W.E.I. Sha, W.C.H. Choy, Y.P. Chen, and W.C. Chew, Appl. Phys. Lett., 99(11), 113304, 2011.
lateral distribution
Bulk heterojunction polymer solar cell

## Slide 8
nanoparticles in spacer layer
nanoparticles in active layer
Comparisons with experimental results
C.C.D. Wang, W.C.H. Choy, etc, J. Mater. Chem., 22, 1206-1211, 2011.
D.D.S. Fung, L.F. Qiao, W.C.H. Choy, etc, J. Mater. Chem., 21, 16349-16356, 2011.
Selected as Back Cover
and Hot Article in
Journal of Material Chemistry

## Slide 9
Dual Plasmonic Nanostructure (experimental results)
power conversion efficiency 8.79%
X.H. Li, W.C.H. Choy, L.J. Huo, F.X. Xie, W.E.I. Sha, B.F. Ding, X. Guo, Y.F. Li, J.H. Hou, J.B. You, and Y. Yang, Adv. Mater., 24, 3046–3052, 2012.
Spin-coating+nanoimprinting

## Slide 10
Shape-Dependent Broadband Plasmonic Resonances
X.H. Li, W.C.H. Choy, H.F. Lu, W.E.I. Sha, and A.H.P Ho, Adv. Funct. Mater., 23(21), 2728–2735, 2013
Ag spherical and triangular nanoparticles

## Slide 11: Could electrical properties of OSCs be affected by introducing the metallic nanostructures?
Wei E. I. Sha, Wallace C. H. Choy and Weng Cho Chew, “Theoretical Studies of Plasmonic Effects in Organic Solar Cells”, Chapter 7, Organic Solar Cells: Materials and Device Physics, Pages 177-210, Wallace C.H. Choy (Ed.), ISBN 978-1-4471-4823-4, Springer, 2013.

## Slide 12: Multiphysics Model (1)
Schematic diagram
W.E.I. Sha, W.C.H. Choy*, Y.M. Wu, and W.C. Chew, Opt. Express, 20(3), 2572-2580, 2012.

## Slide 13: Multiphysics Model (2)
Maxwell’s equation
generation rate
semiconductor equations
Governing equations
exciton dissociation probability
bimolecular recombination rate
frequency dependent permittivity
mobility
Diffusion coefficients
optical electric field
Generation rate
electron density
hole density
electrostatic potential
electrostatic dielectric constant

## Slide 14: Multiphysics Model (3)
Unified finite difference method
optical properties
2D wave equations: TE & TM
spatial step depends on the dielectric wavelength and skin depth of surface plasmons
periodic boundary conditions
stretched-coordinate perfectly matched layer

## Slide 15: Multiphysics Model (4)
electrical properties
Poisson equation (Gummel’s method)
drift-diffusion and continuity equations of electron
(Scharfetter-Gummel scheme in spatial domain
semi-implicit strategy in time domain)
scaling unit
spatial step depends on the Debye length
time step for stable algorithm
Dirichlet and Neumann
boundary conditions

## Slide 16: Multiphysics Model (5)
schematic pattern of nanostrip plasmonic cell
Beyond optical absorption enhancement: facilitating hole collection!
active layer of
standard cell
active layer of
plasmonic cell
(a)
Model settings
active layer thickness
70 nm
periodicity
200 nm
PEDOT:PSS width
100 nm
anode
ohmic
cathode barrier height
0.2 eV
hole mobility
0.1*electron mobility
effective band gap
1.1 eV

## Slide 17: Multiphysics Model (6)
reduce recombination loss
increase short-circuit current
improve open-circuit voltage
boost power conversion efficiency
Characteristic parameters

## Slide 18: Multiphysics Model (7)
Dummy case for further illustrating physics (hole transport and collection)
hole mobility is set to be two order
of magnitude lower than electron mobility
J-V curve
inhomogeneous exciton generation significantly affects
fill factor and
open-circuit voltage

## Slide 19: Multiphysics Model (8)
The nanograting structure v.s. flat standard structure
Simulation parameters

## Slide 20: Multiphysics Model (9)
short-circuit
open-circuit
(a) equipotential lines; (b) recombination rate; (c,d) electron and hole current densities.

## Slide 21: Multiphysics Model (10)
The grating anode induces nonuniform optical absorption and inhomogeneous internal E-field distribution. Thus uneven photocarrier generation and transport are formed in the plasmonic OSC leading to the dropped FF.
recombination and exciton dissociation
Jsc
Voc
W.E.I. Sha, W.C.H. Choy*, and W.C. Chew, Appl. Phys. Lett., 101, 223302, 2012.

## Slide 22: Conclusion
Environmentally friendly organic solar cell (OSC), which has a bright outlook to meet the urgent demand in clean energy, draws much attention in recent years due to their merits of large-area production, low-cost processing and mechanical flexibility. Proposing and optimizing new device architectures plays a key role in designing high-performance OSCs.
A multiphysics study carries out on plasmonic OSCs by solving Maxwell's equations and semiconductor (Poisson, drift-diffusion, and continuity) equations simultaneously with a unified finite-difference framework.
Nonuniform distributions of optical near-fields induced by plasmonic nanostructures will significantly affect the carrier transport in OSCs. Besides their optical effects, the electrical effects induced by plasmonic resonances will open up a new way to design emerging plasmonic organic photovoltaics.

## Slide 23: Acknowledgement
Thanks for your attention!