## Slide 1: Multiphysics Modeling and Understanding for Plasmonic Organic Solar Cells
Department of Electrical and Electronic Engineering,
The University of Hong Kong, Hong Kong
Email: wsha@eee.hku.hk (W.E.I. Sha)
Wei E.I. Sha, Wallace C.H. Choy, and Weng Cho Chew

## Slide 2: Organic Solar Cell (1)
organic solar cell
monocrystalline silicon solar cell
amorphous/polycrystalline silicon solar cell
Advances of solar cell technology

## Slide 3: Organic Solar Cell (2)
Thin-film organic solar cell
low-cost processing
mechanically flexible
large-area application
environmentally friendly
low exciton diffusion length
low carrier mobility

## Slide 4: Organic Solar Cell (3)
optical absorption
exciton diffusion
charge separation
charge collection
Working principle
increase interface area

## Slide 5: Plasmonic Organic Solar Cell
Why optical enhancement?
The thickness of the active layer must be smaller than the exciton diffusion length to avoid bulk recombination. As a result, the thin-film organic solar cell has poor photon absorption or harvesting. Plasmonic solar cell is one of emerging solar cell technologies to enhance the optical absorption.
nanoparticles: local plasmon
nanograting: surface plasmon
Could electrical properties of OSCs be affected by introducing the metallic nanostructures?

## Slide 6: Multiphysics Model (1)
Schematic diagram

## Slide 7: Multiphysics Model (2)
Maxwell’s equation
generation rate
semiconductor equations
Governing equations
exciton dissociation probability
bimolecular recombination rate
frequency dependent permittivity
mobility
Diffusion coefficients
optical electric field
Generation rate
electron density
hole density
electrostatic potential
electrostatic dielectric constant

## Slide 8: Multiphysics Model (3)
Unified finite difference method
optical properties
2D wave equations: TE & TM
spatial step depends on the dielectric wavelength and skin depth of surface plasmons
periodic boundary conditions
stretched-coordinate perfectly matched layer

## Slide 9: Multiphysics Model (4)
electrical properties
Poisson equation (Gummel’s method)
drift-diffusion and continuity equations of electron
(Scharfetter-Gummel scheme in spatial domain
semi-implicit strategy in time domain)
scaling unit
spatial step depends on the Debye length
time step for stable algorithm
Dirichlet and Neumann
boundary conditions

## Slide 10: Multiphysics Model (5)
schematic pattern of nanostrip plasmonic cell
Beyond optical absorption enhancement: facilitating hole collection!
active layer of
standard cell
active layer of
plasmonic cell
(a)
Model settings
active layer thickness
70 nm
periodicity
200 nm
PEDOT:PSS width
100 nm
anode
ohmic
cathode barrier height
0.2 eV
hole mobility
0.1*electron mobility
effective band gap
1.1 eV
W.E.I. Sha, W.C.H. Choy*, Y.M. Wu, and W.C. Chew, Opt. Express, 20(3), 2572-2580, 2012.

## Slide 11: Multiphysics Model (6)
reduce recombination loss
increase short-circuit current
improve open-circuit voltage
boost power conversion efficiency
Characteristic parameters

## Slide 12: Multiphysics Model (7)
Dummy case for further illustrating physics (hole transport and collection)
hole mobility is set to be two order
of magnitude lower than electron mobility
J-V curve
inhomogeneous exciton generation significantly affects
fill factor and
open-circuit voltage

## Slide 13: Multiphysics Model (8)
The nanograting structure v.s. flat standard structure
Simulation parameters
W.E.I. Sha, W.C.H. Choy*, and W.C. Chew, Appl. Phys. Lett., 101, 223302, 2012.

## Slide 14: Multiphysics Model (9)
short-circuit
open-circuit
(a) equipotential lines; (b) recombination rate; (c,d) electron and hole current densities.

## Slide 15: Multiphysics Model (10)
The grating anode induces nonuniform optical absorption and inhomogeneous internal E-field distribution. Thus uneven photocarrier generation and transport are formed in the plasmonic OSC leading to the dropped FF.
recombination and exciton dissociation

## Slide 16: Acknowledgement
Thanks for your attention!